## Slide 1
Thrust 3
Multiple Extremes: General Introduction
Maik Lang, University of Tennessee, mlang2@utk.edu
Elif Ertekin, University of Illinois Urbana-Champaign, ertekin@illinois.edu
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026

## Slide 2
Thrust 3: Multiple Extremes – Outline
Maik Lang/Elif Ertekin – General Introduction of Coupled Extremes
John Hirtz – Radiation Experiments and Defect Characterization
Grady Clopton – Modeling of Ion Track Formation in CeO2 with MD
Amir Movaffagh – Ab initio Modeling of Uranium Carbides and Nitrides
Sara Kadkhodaei – DEF Approach for Defect Phase Diagrams for SHI
Lowell Miyagi – Impact of Defect Structure on Material Behavior at Extremes
Steve Jacobsen – Influence of Defect Structure on Elastic Response
Maik Lang/Elif Ertekin – Facilities, Technique Development and Next Steps
2

## Slide 3
Thrust 3: Multiple Extremes
Goal: To advance our knowledge of the behavior of materials exposed to multiple extreme environments, including intense particle and electromagnetic fields, to enhance material performance and to create new materials.
Modeling – Ion irradiation – Dynamic fragmentation
High-pressure and physical properties
X-ray irradiation and general characterization
3
III. MULTIPLE EXTREMES

## Slide 4
DAC Experiments: Pressure Extremes
4
High pressure synthesis of
hcp CrMnFeCoNi alloy
DAC experiments
High-Pressure Cell P ~ 1 Mbar
C. Tracy, et al.,
Nature Communications (2017)
(CDAC support)
III. MULTIPLE EXTREMES

## Slide 5
High-Temperature Extremes
5
Intense
Laser Pulses
40 J/cm2
from: www.sunbeamtech.com
Phase transitions in ZrO2 from
intense electronic excitations
Ultrafast laser experiments
D.R. Rittman, et al.,
Applied Physics Letters (2015)
(CDAC supported beamtime)
III. MULTIPLE EXTREMES

## Slide 6
Swift Heavy Ions: Extremely Ionizing Radiation
6
Ion Irradiation ρE ~ eV/atom
from: www.simsworkshop.org
Multiple transient extremes within ion tracks
T,P
  Transient energy depositions (~10 eV/atomic bond)
  Intense electronic excitations and extreme ionizations
  Thermal spike with picosecond quenching (~10,000 K)
  Formation of dynamic pressure wave (several GPa)
946 MeV 197Au ions
Galactic Cosmic Rays
Products from Actinide Fissioning
Generated by Heavy Ion Accelerators
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 7
7
Ion Irradiation ρE ~ eV/atom
from: www.simsworkshop.org
Intense
Laser Pulses
40 J/cm2
from: www.sunbeamtech.com
High-Pressure Cell P ~ 1 Mbar
Coupling of Multiple Extremes
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 8
8
M. Lang, et al., Synchrotron Radiation. (2009)
High-Pressure Irradiations
  Relativistic heavy ions penetrate one diamond anvil of DAC (~2 mm)
  Sample is exposed to high pressure (and high-T) when being irradiated
  Successfully applied to 1 Mbar and 1013 ions/cm2
Coupling of Multiple Extremes
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 9
Material Behavior under Coupled Extremes
9
I. Phase Stabilization
Gd2Zr2O7 + 21.5 GPa + 20 GeV Xe ions
M. Lang, et al., Nature Materials (2009)
III. Exotic Molecular Solids
CO2 + 45 GPa + 6 GeV Au ions
II. Phase Transformation
Graphite + 47 GPa + 6 GeV U ions
21.5 GPa
cotunnite
X-Phase
X-Phase
X-Phase
fluorite
graphite
Ice-III
amorphous
cubic diamond
hex. diamond
J.M. Hirtz, et al., in preparation
unpublished data
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 10
Subsequent vs. Simultaneous Coupled Extremes
11
undamaged (cubic)
CeO2
+
Φ
defective (cubic)
P
Φ
P
defective (cubic)
defective (cubic)
high-P phase (orthorhombic)
Φ + P
Subsequent Coupling of Extremes
CeO2 + 35 GPa + 1.7 GeV 197Au ions
Simultaneous Coupling of Extremes
CeO2 + 20 GPa + 7 GeV 238U ions
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 11
Synergistic Effects of Coupled Extremes
10
RBS/C @ TIBML
Rutherford Backscattering (RBS)
  Unique tool for defect analysis
  Depth dependent and highly sensitive
  Ideal for surface and near surface damage
pristine GaN
irradiated GaN
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 12
Modeling Swift, Heavy Ion Irradiation Effects
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
Computational challenge: ion-matter interactions
  Span ~15 orders of magnitude in time (femtoseconds to seconds) and ~8 orders of manitude in length (Angstrom to mm)
  Involves electronic and atomic degrees of freedom that are deeply coupled
  Experiment captures the final state while computation has to reconstruct the pathway
946 MeV 197Au ions

## Slide 13
Molecular Dynamics Approach to SHI Irradiation
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
Bridging electronic energy deposition to atomic dynamics
  SHI deposit enormous energy densities `10s of keV/nm via dense electronic excitation and ionization; classical MD alone insufficient
  Electronic energy coupled to atomic dynamics via electron-phonon coupling, Langevin thermostat, and empirical dose distributions
  Model system: CeO2 where redox effects play a unique role in defect distribution strain evolution, and phase transformation behavior
  A first comprehensive handshake between computation/experiment
CeO2 - G. Clopton (ongoing)
SiO2 – Leino et al. (2015)
Electronic energy deposition to lattice via two-temp molecular dynamics (Darkins et al. 2018)
Notes: Swift heavy ions deposit enormous energy densities (tens of keV/nm) via dense electronic excitation and ionization — classical MD alone cannot capture this Electronic energy coupled to atomic dynamics via: electron-phonon coupling, Langevin thermostat, and empirical dose distributions — approaches validated in UO2, Al2O3, SiC, and pyrochlore CeO2 as model system: redox effects play a unique role in defect distribution, strain evolution, and phase transformation behavior Simulations validated against Lang's experimental benchmark datasets (XANES quantification of redox changes, single ion track characterization) Grain size as a key variable: nano-grained samples show enhanced redox effects, with hypothesized amorphization below 5 nm grain size Deliverable: quantitative, experimentally validated model of ion track formation — portable to other ceramics, metals, and amorphous materials
By contrast, the source term for SHI irradiation (Fig. 2b) is often
assumed to have a two-dimensional Gaussian spatial variation
(width r) and an exponentially decaying time variation (decay
time s)

## Slide 14
Defect Structures and Phase Diagrams
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
From track formation to equilibrium and
metastable defect landscapes
  Molecular dynamics simulations predict the full diversity of defect structures across irradiation conditions: energy density (dE/dx), grain size, pre-existing damage, and dopant concentration
  Defect zoo in irradiated CeO2: Frenkel/Schottky pairs, point defect clusters, dislocation cores, stacking faults, twin boundaries
  Core/shell track morphology: intense plasma-condition core+dilute outer halo; grain size controls competition between oxygen expulsion and grain boundary trapping
  Defect phase diagrams in P-T-m space: map equilibrium and metastable defect phases, identify how coupled extremes shift stability boundaries
Ce2O3
Ia3
Ce7O12
R3
Notes: MD simulations predict the full diversity of defect structures arising across irradiation conditions: energy density (E, dE/dx), grain size, pre-existing damage, and dopant concentration Defect zoo in irradiated CeO2: redox-induced Frenkel/Schottky pairs, point defect clusters, dislocation cores, stacking faults, twin boundaries — and their spatial distributions within and around tracks Core/shell track morphology: inner plasma-condition core with intense damage, outer halo of dilute defects — grain size controls the competition between outward oxygen expulsion and grain boundary trapping Rare earth doping (Sm, Gd, Nd): varying electron/hole concentrations modify the electron-mediated energy transfer, changing defect distributions — experiment and simulation jointly quantify this Defect phase diagrams constructed in P-T-μ space: equilibrium and metastable defect phases, how coupled extremes shift stability boundaries and enable access to otherwise inaccessible defect configurations Framework validated in CeO2, then extended to c-BN, WC, ZrC, ZrN

## Slide 15
From Defects to Mechanical Properties
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
Closing the loop from atomic-scale damage to macroscopic behavior
  MD defect configurations predictions of elastic moduli, yield strength, deformation mechanisms
  Ex: irradiated CeO2 exhibits a 30% strength increase; MD provides the atomistic explanation
  Deformation maps across P-T to ~100 Gpa, 2000 K and strain rates (10-6 yo 102 s-1)
  Framework extended across oxides, carbides. Further: nitrides, amorphous materials, metals ad to P-H, P-E space for hidden phases
SHI effect on strength and texture of CeO2. Courtesy: Lowell Miyagi.
grain size effects

## Slide 16
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026
Radiation Experiments and Defect Characterization
John Hirtz, University of Tennessee, jhirtz@utk.edu

## Slide 17
Radiation Experiments using Swift Heavy Ions
12
17
FAIR – GSI Helmholtz Center (Darmstadt, Germany)
II. Bulk-Irradiation Experiments (Neutron Probes)
~100 mg
M. Lang, et al., Journal of Materials Research (2015)
(CDAC supported)
Sample chambers
diameter: 100 μm
thickness: 25 μm
I. Microscopic Sample Irradiation Experiments (X-ray Probes)
E.C. O’Quinn, et al., Nuclear Science and Engineering (2025)
(CDAC supported)
950 MeV Au ions
1010 – 1014 cm-2
1.5 GeV Au ions
1013 cm-2
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 18
Defect Characterization at Large User Facilities
13
  analysis of large fluence series using 3D-printed customized holder (~1 µg per sample)
  coupled diffraction (XRD) and spectroscopy (EXAFS) measurements
  swelling, strain/grain size, and oxidation state
  developed high-throughput measurement approach, including for actinide materials
X-Ray Analysis at HPCAT
  neutron diffraction & pair distribution function (PDF) analysis
  short- & long-range structural information (cations + anions)
  developing PDF analysis at SNAP: (i) short-range order at high-P (ii) analysis of irradiated samples with reduced mass (~5 mg)
Fourier
transform
Neutron Total Scattering at NOMAD
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 19
Defect Formation in Simple Oxide Fluorites
14
Redox changes induced by ionizing radiation
⇨ partial reduction of Ce4+ to Ce3+
determines radiation response
XRD
Ce K-edge
d = 5.8 ± 0.6 nm
XAS
d = 6.1 ± 0.1 nm
950 MeV Au ions
C.L. Tracy, et al., Nature Communications 6, 6133 (2015)
(CDAC-supported beamtime)
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 20
16
p
e
r
o
x
i
d
e
d
e
f
e
c
t
f
o
r
m
a
t
i
o
n
i
n
C
e
O
2
[
O
—
O
]
2
-
(
o
x
y
g
e
n
-
o
x
y
g
e
n
d
i
s
t
a
n
c
e
~
1
.
4
5
Å
)
R.I. Palomares, et al., J. Mater. Chem. A (2017)
(CDAC supported)
1.5 GeV Au ions
Neutron total scattering and PDF analysis
⇨ peroxide-type O2 clusters formed as counterpart to reduction process (Ce4+ to Ce3+ )
Short-Range Defect Structure in Irradiated Ceria
CeO2
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 21
7
W.F. Cureton, et al., Inorganic Chemistry (2025)
(CDAC supported)
UO2  UO2+x
Short-Range Defect Structure in Oxidized Urania
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 22
17
UC
d = 3 nm
UO2
d = 5 nm
Defect Formation in Oxides versus Carbides
950 MeV Au
Actinide Compounds
Oxidation Behavior
CeO2
ZrC
UC
UO2
ZrC
ZrO2
⇨ direct-impact process for CeO2
⇨ two-step mechanism for ZrC
pristine
irradiated
⇨ less swelling for UO2
⇨ track size UO2 > UC
⇨ oxidation dramatically
in irradiated ZrC
J. Minnette, et al., Journal of Applied Physics (2023)
(CDAC supported)
D. Chaney, et al., Journal of Materials Science (2023)
(CDAC supported)
III. MULTIPLE EXTREMES
Advanced Radiation Facility

## Slide 23
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026
Machine Learned Interatomic Potentials for SHI Irradiation of CeO2
Grady Clopton, University of Illinois Urbana-Champaign, gclopton@illinois.edu

## Slide 24
Classical MD Results
SHI Track simulations in LAMMPS with classical rigid-ion Buckingham + Coulomb potential
Simulations captured thermal disorder, point defects, and local rearrangements; did not reproduce the chemically realistic track response suggested by experiment
Core Limitation: fixed-charge classical potentials cannot represent Ce(4+) → Ce(3+) reduction.
Oxygen vacancy formation in real ceria leaves two electrons that localize on nearby Ce sites; this changes local bonding, defect energetics, migration barriers, strain, and recovery behavior.

## Slide 25
MLIP Generation
25
MLIP trained on first-principles energies and forces
The MLIP learns not just distances, but the geometry of the local coordination environment.
makes large-scale TTM-MD in LAMMPS, practical
Training strategy: calibrate a consistent DFT+U reference, then generate labeled structures across the ceria reduction series
Train on DFT+U energies, forces, and stresses

## Slide 26
Data Generation
Main challenge: in ceria, oxygen vacancies are coupled to Ce⁴⁺/Ce³⁺ redox changes
Training data must therefore capture both atomic distortions and the correct localized 4f electronic state
DFT+U can describe this physics, but reduced ceria often has multiple metastable 4f occupation patterns
We generate data across the ceria reduction series CeO₂, Ce₇O₁₂ Ce₂O₃.
Data Generation Process:
  Use ab initio molecular dynamics at multiple temperatures to sample anharmonic, non-equilibrium local environments
  Label each configuration with total energies, atomic forces

## Slide 27
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026
Ab initio Modeling of Uranium Carbides and Nitrides
Amir O. Movaffagh, University of Illinois Chicago, aorvat2@uic.edu

## Slide 28
Actinide Ceramics for Advanced Reactor Fuel Applications
Jacob Minnette
Amir M. Orvati Movaffagh
III. MULTIPLE EXTREMES
Targeted Materials
Carbothermic Reduction
Reaction
UO3
UC
UN
MOTIVATION
Synthesis and multi-scale characterization of UC and UN TRISO fuel kernels for application in accident tolerant fuel (ATF) systems via sol–gel internal gelation
SIGNIFICANCE
Multiple rocksalt UN (UCN) phases identirfied, enabled by high-resolution XRD/neutron scattering
Improved control of phase composition in UC/UN TRISO fuel kernels through synthesis–structure relationships
Scalable production of uniform TRISO fuel kernels with controlled microstructure

## Slide 29
Jacob Minnette
Amir M. Orvati Movaffagh
III. MULTIPLE EXTREMES
Targeted Materials
Challenges:
Anion-site composition: identification of species occupying N-sites
Multiple rocksalt phases: Underlying mechanisms behind the formation of UN-1 and UN-2
Oxidation behavior: Relative stability and reaction pathways of UC vs. UC₂ and UN vs. U₂N₃
Refinement parameter | X-ray | Neutron
Rocksalt (UN-1) [wt. %] | 67.4 ± 0.6 | 69.6 ± 0.7 *
Rocksalt (UN-2) [wt. %] | 28.5 ± 0.6 | 25.8 ± 0.7 *
Actinide Ceramics for Advanced Reactor Fuel Applications

## Slide 30
Jacob Minnette
Amir M. Orvati Movaffagh
III. MULTIPLE EXTREMES
Targeted Materials
Actinide Ceramics for Advanced Reactor Fuel Applications
At 50%:
SQS - VCA ≈ 0.2%
+0.43%
+0.10%
+0.25%
+0.46%
-0.65%
+0.25%
+0.69%
+0.63%
+0.25%
+0.69%
+0.35%
+0.22%
-0.16%
+0.35%
+0.22%
≈ 99.5% Accuracy
Results so far:
SQS reproduces UCP with ~99.5% accuracy
UCP curvature explained: Attributed to carbon incorporation on N-sites and local chemical environment effects, not captured by VCA
SQS
VCA

## Slide 31
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026
DEF Approach for Defect Phase Diagrams for SHI
Sara Kadkhodaei, Ph.D.
Associate Professor,
University of Illinois Chicago, sarakad@uic.edu

## Slide 32
Ab initio Modeling of Defects
32
III. MULTIPLE EXTREMES
Experiment and Theory
LIMITATION
Chemical potential (μ)- and Fermi level (ΕF)- dependent defect energetics
Defects are typically treated individually, without a unified description of their collective distribution in defective phases
I. DFT calculations of defects in ceria
II. Defect energies in UC
Ertekin’s group (ongoing)
Huang, J. Phys. Chem. C, 2010| Zacherle, Phys. Rev. B. 2013 |Tiwary, Phys. Rev. B. 2009| Ducher, Phys. Rev. B. 2011

## Slide 33
CALPHAD Modeling of Defects
33
III. MULTIPLE EXTREMES
Experiment and Theory
LIMITATION
Phase diagrams often rely on fitting thermochemical data
Built from heat capacities and measured phase boundaries
Data-dependent and non-universal, limited physical grounding
Phase-boundary data are hard to obtain for dilute defects
Does not identify defect types (blind to defect chemistry)
ADVANTAGE
Environment-independent Gibbs energy (G) parameterization
Chemical and electronic coexistence conditions come directly from CALPHAD
No separate deduction needed for varying T, X, and P.
Matvei Zinkevich, et al., Solid State Ionics 177 (2006)
CALPHAD
Phase diagram of Ce-O around CeO2
Lian Cheng Wang, (2018)

## Slide 34
Defect Energy Formalism (DEF)
34
III. MULTIPLE EXTREMES
Experiment and Theory
MOTIVATION
Integrating ab initio defect energetics into CALPHAD Gibbs energies with predictive advantages
  collective descriptions of defects in defective phases
  Universal parameterization independent of μ and EF
I. Physics-grounded Gibbs Energy of Defective Phases in DEF
A. Movaffagh, et al., Physical Review Materials 8 (2024)
II. Application of DEF to dilute defect thermodynamics in Mg2Si
A. Movaffagh, et al., submitted to Acta Materialia (2026),

## Slide 35
MOTIVATION
Investigate irradiation-induced defects in CeO₂ and the resulting microstructural and phase changes
APPROACH
A combined theoretical, modeling, and experimental approach
Intense ion irradiation at a large accelerator facility (Lang, UTK)
Ab initio/MLIP molecular dynamics simulation (Ertekin, UIUC)
DEF analysis of defective phases (Kadkhodaei, UIC)
Sara Kadkhodaei
Elif Ertekin
Maik Lang
DEF Analysis of SHI Tracks and Phase Tolerance in Ceria
III. MULTIPLE EXTREMES
Experiment and Theory
Ertekin’s group (ongoing)
⇨ peroxide-type O2 clusters formed as counter part to reduction process (Ce4+ to Ce3+ )
II. Two-temperature MD simulation of ion irradiation in ceria
I. Neutron total scattering and PDF
R.I. Palomares, et al., J. Mater. Chem. A (2017)
DEF for Modeling
Incorporating defect complexes (e.g., peroxide-type dimer, oxygen Frenkel pairs)
Ordering of oxygen vacancies can produce locally ordered fluorite-derivative superstructures that break from long-range fluorite symmetry
Notes: The goal of this collaborative research is to investigate the behavior of radiation defects in ceria using a combined theoretical, computational, machine-learning, and experimental framework.
Top figure: an example of an irradiation ion track in ceria
Bottom figure: a snapshot of two-temperature MD simulation of ion irradiation in ceria (Ertekin’s group)
- Right figure: an example of a CALPHAD-based phase diagram of Ce-O, illustrating non-stoichiometric ceria (fluorite phase) and several locally ordered fluorite-derivative superstructures

## Slide 36
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026
Impact of Defect Structure on
Material Behavior at Extremes
Lowell Miyagi, Ph.D.
Professor,
University of Utah, lowell.miyagi@utah.edu

## Slide 37
Impact of Defect Structure on Materials Behavior Under Extremes
Elif Ertekin
Maik Lang
Steve Jacobsen
J. Hirtz (UTK), R. Hrubiak (HP-CAT), and A. Berlin (UU)
Sector 16-ID-B
Lowell Miyagi
Chantelle Kiessner
Blake Sturtevant
LANL

## Slide 38
Radial Diffraction
Crystal lattice strain (elastic)
  Calculate stresses
  Strength of materials
Texture / preferred orientation (plastic)
  Deformation mechanisms (slip systems, twinning)
  Transformation mechanisms

## Slide 39
Polycrystal Plasticity Modeling → Deformation Mechanisms
b
a
VPSC models
Visco-plastic self consistent code (Lebensohn and Tome 1993)
Self consistent modeling
Elasto-plastic self consistent code (Turner and Tome 1993; Merkel et al 2009)
EVPSC
(Wang et al 2010)
Applied to
high pressure
(Lin et al., 2017)
Carlos Tomé
Ricardo Lebensohn

## Slide 40
Experiment
EVPSC
Deformation of CeO2 Cerianite (Huston et al., 2022)
Pratt et al 1966 - fluorite primary slip system is {100}<110>
FCC metals – slip on {111}<1-10>
Notes: Note {100}<110> also gives a 011 texture but the Q don’t fit

## Slide 41
Deformation of Irradiated CeO2 Cerianite (200 MeV Xe )
{110}<1-11>
{112}<111> twinning
Notes: Shear modulus from Sun et al., 2010

## Slide 42
Berlin in prep
Kiessner et al., in prep
Radiation damage in nano and micro CeO2
Grain size reduction increases strength
Grain size reduction changes deformation mechanisms (increased twinning)
Irradiated samples are stronger
Radiation damage changes deformation mechanisms (suppresses twinning)
Mechanism of strengthening in irradiated samples is distinct from grain size reduction
Impact of Defect Structure on Materials Behavior Under Extremes
What about other materials?
  CDAC student A. Berlin.
  WC irradiated with 946 MeV 197Au ions.
Future work:
  Defect modeling materials (Ertikin)
  Elasticity measurements (Jacobsen).

## Slide 43
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026
Influence of Defect Structure on Elastic Response
Steven Jacobsen, Ph.D.
Professor,
University of Colorado, Boulder, steven.jacobsen@colorado.edu
Influence of Defect Structure on Elastic Response

## Slide 44
GHz-ultrasonics: a unique capability of the Center
I. MULTIPLE EXTREMES
Future Directions
MOTIVATION
Measure high-precision acoustic velocities in samples that are too small or opaque for conventional methods (MHz-ultrasonics, Brillouin): Irradiated samples and deformation experiments
APPROACH
100mm diameter probe
P-to-S conversion
In conjunction with sample-length interferometry, we can use GHz P-wave and S-wave measurements to determine highly accurate elastic constants in sub-mm crystals, glasses, and nanopolycrystalline materials.
Developed thin-film ZnO transducers to produce acoustic waves with near-optical wavelength at 1-2 GHz

## Slide 45
I. MULTIPLE EXTREMES
Future Directions
GHz-ultrasonics: a unique capability of the Center
Acetaminophen
(RDX analog) elastic tensor
Anomalous compression of v-SiO2
NPD
Opaque Crystals
Molecular Crystals
Superhard Materials
Nanocrystalline Materials
Chang et al. (2014) PEPI 228:47
Liu et al. (2017) Sci Rep 7:42921
Jacobsen et al. (2004) PNAS 101:5867
(note: this study shown because it informs the current ZFSP project)
Amorphous Materials
Clark et al. (2014) PRB 90:174110
In collaboration with K. Ramos and C. Bolme, LANL (work in prep)
FUTURE DIRECTION
CDAC Partners Jacobsen (CU Boulder), Lowell Miyagi (Utah) and Maik Lang (Tennessee) plan to collaborate on using GHz-ultrasonics to determine the ambient shear modulus for dynamic-DAC data interpretation, deformation experiments, and irradiated samples

## Slide 46
Thrust 3
Multiple Extremes: Technique Development; Next Steps
Maik Lang, University of Tennessee, mlang2@utk.edu
Elif Ertekin, University of Illinois Urbana-Champaign, ertekin@illinois.edu
Stewardship Science
Academic Alliances
Center Review Meeting
April 15, 2026

## Slide 47
Advanced Approach to Couple Extremes
7
III. MULTIPLE EXTREMES
Advanced Radiation Facility
2 mm
Synchrotron XRD: amorphization of ice III
Molecular amorphous CO2 phase?
CO2
Synchrotron-IR measurements of CO2
7 GeV 238U ions
45 GPa
Raman
IR
I. Tzifas et al., Physical Review research (2026)
(CDAC supported)

## Slide 48
Coupling High-Pressure with Displacive Damage
7
III. MULTIPLE EXTREMES
Advanced Radiation Facility
MOTIVATION
Simulate defective microstructure from self-decay of actinides and test impact on high-pressure and high-temperature behavior
APPROACH
Need low-energy accelerator facility
Determine dose level profile and optimize displacive damage within microscopic sample
Perform high-pressure/temperature experiments after ion-beam exposure at HPCAT
Correlate experimental results with model predictions
Significance
First assessment of how defects and a damaged microstructure affect material behavior under extremes
Refinement and expansion of existing equilibrium phase diagrams that are only based on pristine materials
Important data to predict impact of actinide delf-decay on phase stability and behavior under extremes
Insight whether defect engineering can be used to enhance materials resistance under extremes
Essential training opportunity for students in key field

## Slide 49
Developing Neutron Scattering for Small Samples
7
III. MULTIPLE EXTREMES
Advanced Radiation Facility
MOTIVATION
Enable neutron total scattering and PDF analysis for small sample quantities to (i) obtain short-range order information with sensitivity to both cations and anions, and (ii) enable high-throughput studies of irradiated materials
APPROACH
Utilize existing SNAP facility at SNS currently utilized only for diffraction experiments (focused neutron beam)
Develop background removal procedures to obtain useable total scattering data
Test applicability to diamond anvil cells, capillaries, and microscopic ion-beam sample holders
Significance
Significant enhancement of advanced structural characterization of ion irradiated materials
Sample minimization allows measurement of highly radioactive materials
Short-range order accessible for high-pressure studies to better understand impact on phase transformations
Sample chambers
diameter: 100 μm
thickness: 25 μm
mass: ~1 µg
950 MeV Au ions
1010 – 1014 cm-2
Sample chambers
diameter: 9 x 1 cm
thickness: 25 μm
mass: ~100 mg
1.5 GeV Au ions
1013 cm-2
X-Rays Neutrons
A2B2O7
E.C. O’Quinn, et al., Nuclear Science and Engineering (2025)
(CDAC supported)
pristine 6 GPa
irradiated - ambient

## Slide 50
Foundation MLIPs for Redox-Active Materials
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
MOTIVATION
Classical potentials cannot capture Ce³⁺/Ce⁴⁺ redox effects; accurate defect structures require charge/spin-aware MLIPs
APPROACH
Develop transferable neural network MLIP for CeO2 with explicit oxidation state
Neural network cluster expansion on GPU: long-timescale MD with spin/oxidation state degrees of freedom
Couple to two-temperature model for electron-phonon dynamics at ion-track timescales
Pretrain across compositions and damage conditions; fine-tune to specific irradiation regimes
Significance
First charge/spin-aware MLIP for redox-active ceramics validated against experimental observables
Foundation model portable to other REE-oxides and actinide systems
Prerequisite for reliable defect phase diagram construction and mechanical property prediction
Training opportunity at the intersection of ML, atomic simulation, and extreme-condition materials

## Slide 51
Exp-Driven MLIP Refinement, AI Accelerated Sampling
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
MOTIVATION
MD cannot exhaustively cover the high-dimensional coupled extreme condition space — experiment and computation must inform each other continuously
APPROACH
XANES measurements of Ce³⁺/Ce⁴⁺ redox changes as quantitative update signal for MLIP refinement
Symmetry-decomposed representations to characterize correlated disorder in MD snapshots
Surrogate models trained on validated MD snapshots for accelerated condition space sampling
Active learning prioritizes most informative (P, T, dE/dx, grain size) combinations
Significance
Quantitative, automated feedback loop between XANES data and atomistic models
Symmetry-decomposed disorder descriptors: physically interpretable, transferable across material classes
Dramatic reduction in computational cost of condition space exploration
XANES measurements:
Quantify Ce3+/Ce4+
MLIP parameter updates; subsequent MD
Symmetry-decomposed analysis of MD damage profiles

## Slide 52
Toward Autonomous Discovery of Hidden Phases
11
III. MULTIPLE EXTREMES
Advanced Radiation Facility
MOTIVATION
The coupled P-T-H-E condition space is vast — sequential human-guided exploration cannot efficiently locate hidden and metastable phases
APPROACH
Model-to-experiment: AI predictions guide irradiation experiments toward conditions most likely to yield hidden phases
Experiment-to-model: XANES and diffraction data update models continuously
One-shot damage structure generation: Feynman-Kac steering in diffusion models (early-stage work in progress)
Longer horizon: fully autonomous laboratory across P-T-H-E space
Significance
First closed-loop AI-driven discovery in coupled extreme condition space
Feynman-Kac/diffusion approach: physically grounded generative framework for disordered materials
Active learning protocol transferable to other CDAC material classes and condition combinations
Positions CDAC uniquely at the intersection of world-unique experiments and Genesis AI/ML framework
Training opportunity at the frontier of AI for materials discovery