# Modeling of Uranium Carbide and Uranium Nitride Fuel Kernels (slides 28-30)

- This collaborative project combines advanced experimental characterization and density functional theory (DFT) modeling to study uranium carbide (UC) and uranium nitride (UN) fuel kernels produced for potential use in accident-tolerant TRISO fuels for next-generation, high-temperature reactors.

- High-resolution synchrotron X-ray scattering at NSLS-II, Brookhaven National Laboratory, and spallation-neutron total scattering using NOMAD at Oak Ridge National Laboratory identified three phases in the UN kernels. Rietveld refinement of the neutron diffraction data yielded 69.6 wt.% UN-1, 25.8 wt.% UN-2, and 4.6 wt.% α-U₂N₃, with lattice parameters of approximately 4.901 and 4.911 Å for UN-1 and UN-2, respectively (slide 29, left figure). These subphases may arise from differences in the identities or concentrations of impurities incorporated during carbothermic reduction.

- DFT calculations were therefore performed to test whether carbon substitution on the nitrogen sublattice could independently reproduce the experimentally observed nonlinear relationship between lattice parameter and composition. The calculations reproduced both the magnitude and curvature of the experimental trend (slide 30, top left figure), supporting carbon substitution as a principal contributor to the expanded UN lattice.

- Special quasirandom structures (SQS), which explicitly represent carbon–nitrogen disorder on the anion sublattice, reproduced the experimentally observed nonlinear composition dependence, whereas the compositionally averaged virtual crystal approximation (VCA) predicted nearly Vegard-like behavior. The maximum lattice-parameter difference between the methods was approximately 0.2%, indicating that local atomic-environment effects make a small but measurable contribution to the deviation from Vegard’s law.

- Partial radial-distribution-function analysis (slide 30, right figure) attributes the SQS–VCA discrepancy to differences in their representation of local atomic environments. At 50% carbon substitution, an approximately 0.2% shift in the third-neighbor peak positions is observed between the SQS and VCA atomic-pair distributions, consistent with the approximately 0.2% difference in their predicted lattice parameters. This correspondence indicates that the non-Vegard behavior captured by SQS originates from local structural relaxation that is absent from the compositionally averaged VCA.

- Ongoing work will investigate the thermodynamic and structural mechanisms responsible for the formation of UN-1 and UN-2 and determine whether their different lattice parameters arise solely from carbon concentration or also reflect oxygen incorporation, nitrogen vacancies, or other synthesis-dependent effects.